## Slide 1: Optical Filters for Life science applications
Mike Scobey
Alluxa Inc.

## Slide 2: Alluxa Inc.
Santa Rosa, California.
8 years old, growing steadily, now with 55 employees with 20 engineers
Proprietary SIRRUS plasma PVD deposition process
In house chamber process design/development
10 identical, state-of-the-art plasma deposition chambers and growing
24x7, fully automated operation with clean operations throughout

## Slide 3: Thin film optical filters
QW = l0/4
nQW
High Index
Low Index
Principle of constructive and destructive interference
Alluxa films are all hard-oxide and extraordinarily environmentally durable.
Modern filters may have up to 400 layers

## Slide 4: Common types of optical filters
Type | Layers | Function/Description | Typical Tolerances (+/-)
AR | 1 to 20 | Suppress reflection | 5-10%
HR | 30 to 150 | High reflection across a band | 2-5%
Bandpass | 60 to 250 | Transmit one band, reject all others on each side | 0.5% to 5%
Multi-bandpass | 200-400 | Transmit multiple bands, reject all others | 0.25% to 1%
Edge filter | 40-200 | Transmit one band, rejects adjacent bands | 0.5% to 5%
Dichroic | 50-150 | Tilted edge filter. Generally requires flatness | 0.5% to 2%
Notch | 200-500 | Reject narrow band, transmit all others | 0.25% to 1%
Multi-notch | 400-2000 | Reject multiple narrow bands, transmit all others | 0.25% to 1%

## Slide 5: Sirrus Deposition platform
Proprietary to Alluxa
High energy plasma PVD
Extraordinarily durable, hard oxide coatings
Virtually no scatter or absorption loss
Fastest deposition in the industry enables lower price points and higher performance
Ultra-precise layer deposition using proprietary optical monitoring and control systems
Copy exact – 10 chambers

## Slide 6: Alluxa’s Ultra Series Optical Filters
Parameter | Alluxa ULTRA | Leading competitor | Notes
Transmission | 95% | 92% | Alluxa typical is 98%
Blocking | Broadband OD6 to OD10 | OD6 but over narrow bands with OD10 available | Measurement limited at OD6
CWL control | +/-1.5nm or less | +/-3nm | Key for S/N and lower bleed thru
Slopes | 0.5% to OD6 | 1% to OD5 best case | Coupled with CWL control gives much improved bleed thru and crosstalk

## Slide 7: Ultra Series BP for Life
Performance leader with repeatable >95% transmission, ultra-tight wavelength control and wide OD6 out-of-band blocking

## Slide 8: Ultra-series Multi-band EX and EM filter

## Slide 9: Fluorescence Microscopy
Requires non-overlapping bandpass filters with high blocking for excitation and emission
Dichroic filter for beam steering

## Slide 10: Typical Ultra fluorescence Filter Set

## Slide 11: Fluoresce Microscopy images
Kidney
Chinese
Hamster Ovary

## Slide 12: LED Illuminators
Gaining share in microscopy as well as OEM instruments
Energy efficient and rapid on/off
Mercury free, long life
Dichroic filters and precision bandpass filters

## Slide 13: Ultra flat dichroics

## Slide 14: Confocal Microscopy

## Slide 15: ULTRA Quad-chroics for confocal Microscopy
Ultra-flat available

## Slide 16: Multiphoton Microscopy
From Nikon U

## Slide 17: Structured illumination
Super resolution techniques to defeat the diffraction limit
Dichroics, Bandpass, phase controlled mirrors, among others

## Slide 18: stimulated emission depletion (STED) microscope
BPF
VPP
P
QWP
Objective
QWP
DCSP
DCLP
NF
PH
APD
BPF
l 592 nm
l 488 nm
Excitation Beam
Depletion Beam
STED Image

## Slide 19: Images using STED Super resolution
HELA Telophase
Chromosome bands

## Slide 20: Flow cytometry
Single cell counting and sorting
Single and multiband dichroics, bandpass, narrowband filters

## Slide 21: Flow Cytometry Ultra multibands

## Slide 22: PCR systems
DNA amplification for analysis
Dichroics, bandpass, narrowband filters

## Slide 23: ULTRA Multi-Bandpass EMission Filters

## Slide 24: Multiband microscopy results
Taken using Alluxa Quad Band Dichroic and Tri-Band EM Filters

## Slide 25: Automation and process control enables repeatability

## Slide 26: ULTRA UV Band Pass Filters

## Slide 27: fluorescence with visible imaging filter

## Slide 28: Rapid turn custom filters
Catalog quadchroic converted to a penta-band
Order, design, fab in < 4 weeks
Competitor
Added 5th notch

## Slide 29: Ultra-narrow Multicavity BP’s
Bandwidths to <0.2nm with large formats available.
Multicavity designs for square spectral performance
Unique product offering of bandwidth and size
63 wavelengths now shipping from our new on-line store

## Slide 30: Really Ultra Narrow!

## Slide 31: Ultra narrow OD6 Notch Filters with wide transmission

## Slide 32: Color corrected notch for laser surgery

## Slide 33: Raman 785nm LWP

## Slide 34: Low cost LED edge Filters for forensics
Consumable for flashlights at crime scene investigation

## Slide 35: Low Cost Catalog OD4 Filters

## Slide 36: Arbitrary shape filters

## Slide 37: Summary
Innumerable applications for optical filters in Life Sciences
Rapidly developing coating technologies are pushing the state of the art
The SIRRUS deposition platform enables Alluxa to be at forefront of performance while improving price points
Alluxa is always up for new challenges!